**FOOD BUDDY PRODUCT SPECIFICATIONS**

**A picture containing handwear, clothing, indoor

Description generated with very high confidence**

**Name of Product** - 9.0 Mil Powder Free Heavy Duty Nitrile Gloves.

**Name of Manufacturer**  - Innovative Gloves Co. Ltd. Hatyai, Thailand.

**Base Material**  - Nitrile.

**Characteristics** -Non-Sterile, Ambidextrous Beaded Cuff.

**Available Sizes** - Small(7), Medium(8), Large(9), X-Large(10), XX-Large(11).

**Surface** - Diamond Textured.

**Surface Treatment** - Polymer Coating.

**Color**  - Dark Blue/Yellow.

**Total Residue Content** - < 2.0 Milligrams per glove.

**Physical Specifications:**

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| **Size** | **Length(mm/inch)** | **Thickness(mm)**  **Single Wall** | | | | **Width(mm)** |
| Finger Tip  Smooth surface | Finger Tip  Textured Surface | Palm | Cuff |
| Small(7) | 300±10 | 0.24±0.01 | 0.40±0.02 | 0.45±0.02 | 0.12±0.01 | 85±5 |
| Medium(8) | 300±10 | 0.24±0.01 | 0.40±0.02 | 0.45±0.02 | 0.12±0.01 | 95±5 |
| Large(9) | 300±10 | 0.24±0.01 | 0.40±0.02 | 0.45±0.02 | 0.12±0.01 | 105±5 |
| X-Large(10) | 300±10 | 0.24±0.01 | 0.40±0.02 | 0.45±0.02 | 0.12±0.01 | 115±5 |
| XX-Large(11) | 300±10 | 0.24±0.01 | 0.40±0.02 | 0.45±0.02 | 0.12±0.01 | 120±3 |

**Tensile (ASTM D412 & EN 455-2)**

**Before Aging**

|  |  |  |
| --- | --- | --- |
| **Tensile(MPA)** | **Elongation(%)** | **Force At Break(N)** |
| 22 Mpa Min. | 500 Min. | ≥ 6 N |

**After Accelerated Aging**

|  |  |  |
| --- | --- | --- |
| **Tensile(MPA)** | **Elongation(%)** | **Force At Break(N)** |
| 22 Mpa Min. | 400 Min. | ≥ 6 N |

**Packaging**

|  |  |
| --- | --- |
| **Packaging (Normal)** | 50±1 pieces in one Poly Bag or Inner Box,10 Poly Bag or Innr Box in one Carton. |
| **Labeling on Dispenser (Normal)** | Product Name, Size, Lot no. Quantity, Manufacturer’s address. |
| **Labeling on Carton (Normal)** | Product Name, Size, Lot no. Quantity, Country of Origin. |

**Container Loadability** (No MOQ in manufacturer owned brand in standard Packaging)

|  |  |
| --- | --- |
| 20 FCL=985 Cartons. | 40 FCL=1990 Cartons. |

,

**Certification**

A close up of a sign

Description generated with very high confidence