**SILVER LINE PRODUCT SPECIFICATIONS**

A picture containing handwear, clothing

Description generated with very high confidence

**Name of Product** - 14 Mil Powder free Latex House Hold Gloves.

**Name of Manufacturer**  - Innovative Gloves Co. Ltd. Hatyai, Thailand.

**Base Material**  - Natural Rubber Latex.

**Characteristics** -Non-Sterile, Ambidextrous Beaded Cuff.

**Available Sizes** - Small, Medium, Large, X-Large, XX-Large.

**Surface** - Diamond Textured.

**Surface Treatment** - Mild Washing with Chlorine Solution and Extensive Washing.

**Color**  - White/Blue.

**Total Residue Content** - < 2.0 Milligrams per glove.

**Total Extractable** - < 50µ gram/ gram of glove

**protein content**

**Physical Specifications:**

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Size** | **Length(mm/inch)** |  | | **Thickness(mm)**  **Single Wall** | | | **Width(mm)** |
| Tip Smooth Surface | Tip Textured Surface | | Palm Textured Surface | Cuff Smooth Surface |
| Small(7) | 300±10 | 0.37±0.01 | 0.66±0.02 | | 0.74±0.02 | 0.21±0.01 | 95±5 |
| Medium(8) | 300±10 | 0.37±0.01 | 0.66±0.02 | | 0.74±0.02 | 0.21±0.01 | 100±5 |
| Large(9) | 300±10 | 0.37±0.01 | 0.66±0.02 | | 0.74±0.02 | 0.21±0.01 | 115±5 |
| X-Large(10) | 300±10 | 0.37±0.01 | 0.66±0.02 | | 0.74±0.02 | 0.21±0.01 | 120±3 |
| XX-Large(11) | 300±10 | 0.37±0.01 | 0.66±0.02 | | 0.74±0.02 | 0.21±0.01 | 125±3 |

**Tensile (ASTM D412 & EN 455-2)**

**Before Aging**

|  |  |  |
| --- | --- | --- |
| **Tensile(MPA)** | **Elongation(%)** | **Force At Break(N)** |
| 21 Mpa Min. | 700 Min. | ≥ 6 N |

**After Accelerated Aging**

|  |  |  |
| --- | --- | --- |
| **Tensile(MPA)** | **Elongation(%)** | **Force At Break(N)** |
| 18 Mpa Min. | 500 Min. | ≥ 6 N |

**Packaging**

|  |  |
| --- | --- |
| **Packaging (Normal)** | 50±1 pieces in one Dispenser Box or Poly Bag,10 Dispenser Box or Poly Bag in one Carton. |
| **Labeling on Dispenser (Normal)** | Product Name, Size, Lot no. Quantity, Manufacturer’s address,Warning about Latex Allergy. |
| **Labeling on Carton (Normal)** | Product Name, Size, Lot no. Quantity, Country of Origin. |

**Container Loadability** (No MOQ in manufacturer owned brand in standard Packaging)

|  |  |
| --- | --- |
| 20 FCL=627 Cartons. | 40 FCL=1260 Cartons. |

,

**Certification**

**A drawing of a person

Description generated with high confidence**