**FOOD BUDDY PRODUCT SPECIFICATIONS**

**A picture containing handwear, clothing

Description generated with very high confidenceName of Product** : **9.0 Mil Powder Free Heavy Duty Nitrile Gloves.**

**Name of Manufacturer** : Innovative Gloves Co. Ltd. Hatyai, Thailand

**Base Material** : Nitriles

**Characteristics**  :Non Sterile, Ambidextrous Beaded Cuff.

**Available Sizes** :Small(7),Medium(8),Large(9),X-Large(10),XX-Large(11)

**Surface** :Diamond Textured.

**Surface Treatment** :Polymer Coating

**Colour**  :Dark Blue.

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Physical Specifications:** | | | | | |  | | |  |  |  |  |  |  |  | | |  |  |  |  |  |  |
|  |  |  | Length | |  |  |  | SINGLE WALL (mm) | | | | | | | | | | | | |  | Width |  |
|  | Size | |  | Finger Tip | | |  |  | Finger Tip | |  |  | Palm | | |  |  | Cuff | |  |
|  | (mm) | |  |  |  |  |  |  | | |  |  | (mm) |  |
|  |  |  |  | Textured Surface | | |  |  | Smooth | |  |  |  | | Textured | | | | Smooth |  |
|  |  |  |  |  |  |  |  |  |  |  | |  |  |
|  |  |  |  |  |  |  | | |  |  | Surface | |  |  |  | | Surface | | | | Surface |  |  |
|  | Small (7) | | 310±15 | |  | 0.40±0.05 | | |  |  | 0.24±0.01 | |  |  | | 0.45±0.05 | | | | | 0.12±0.01 | 85±5 |  |
|  |  | |  | |  |  | | |  |  |  | |  |  | |  | | | | |  |  |  |
|  | Medium (8) | | 310±15 | |  | 0.40±0.05 | | |  |  | 0.24±0.01 | |  |  | | 0.45±0.05 | | | | | 0.12±0.01 | 95±5 |  |
|  |  | |  | |  |  | | |  |  |  | |  |  | |  | | | | |  |  |  |
|  | Large (9) | | 310±15 | |  | 0.40±0.05 | | |  |  | 0.24±0.01 | |  |  | | 0.45±0.05 | | | | | 0.12±0.01 | 105±5 |  |
|  | X Large (10) | | 310±15 | |  | 0.40±0.05 | | |  |  | 0.24±0.01 | |  |  | | 0.45±0.05 | | | | | 0.12±0.01 | 115±5 |  |
|  | XX Large (11) | | 310±15 | |  | 0.40±0.05 | | |  |  | 0.24±0.01 | |  |  | | 0.45±0.05 | | | | | 0.12±0.01 | 125±5 |  |

|  |  |  |
| --- | --- | --- |
| **Tensile(MPA)** | **Elongation(%)** | **Force At Break(N)** |
| **22 Mpa(A/A)** | **400% min.(A/A)** | **7 N** |

**Tensile (ASTM D 6319 & EN 455-2)**

**Quality Assurance**

|  |  |
| --- | --- |
| **Visual Inspection G-I AQL** | **Physical dimension S-II AQL** |
| **Leak Test G-I AQL** | **Physical Properties S-II AQL** |

**Packaging**

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Total Residue Content** | | | | |  |  | - < 2.0 Milligrams per glove | |
| **Packaging (Normal)** | | | | |  |  | - 50 pieces in one Poly Bag or Inner Box | | |
|  |  |  |  |  |  |  | 10 Poly Bags or Inner Box in one Carton | | |
| **Labeling on Polybag (Normal)** | | | | | | | - Product Name, Size, |
| **Labeling on Carton (Normal)** | | | | | | | - Product Name, Size, Lot no. Quantity, | | |
|  |  |  |  |  |  |  | Country of Origin |

**Container Load ability** (No MOQ in manufacturer owned brand in standard Packaging)

20FCL=985 Cartons,40 FCL=1990 Cartons.