**HIGH RISK PRODUCT SPECIFICATIONS**

|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | **Name of Product** | |  |  |  | : **14.0 Mil Powder Free Latex High Risk Gloves.** | | | | | |
|  | **Name of Manufacturer** : :Innovative Gloves Co. Ltd. Hatyai, Thailand | | | | | | | | | |
|  | **Base Material** | | |  |  | : Natural Latex | | |  |
|  | **Characteristics** | | |  |  | : Non Sterile, Ambidextrous Beaded Cuff | | | | |
|  | **Available Sizes** | | |  |  | : Small, Medium, Large, X-Large, XX- Large | | | | |
|  | **Surface** |  |  |  |  | : Diamond Textured. | | | |
|  | **Surface Treatment** | | | | | **:** Mild washing with chlorine solution and extensive | | | | | |
|  | **Colour** |  |  |  |  | Washing. |  |  |  |
|  |  |  |  |  | : Blue. | | |  |

A picture containing clothing, handwear

Description generated with very high confidence

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Physical Specifications:** | | | | | |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Length | |  | SINGLE WALL (mm) | | | | | | | | |  |  |
|  | Size | |  | Cuff |  | Palm | |  |  |  |  | Tip | |  |
|  | (mm) | |  |  |  |  |  |  |  |
|  |  |  |  | Smooth |  | Textured | |  |  | Textured | | | Width(mm) |  |
|  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | Surface |  | Surface | |  |  | Surface | | |  |  |
|  | Small | | 300±10 | |  | 0.21±0.01 |  | 0.28±0.01 | |  | 0.37±.001 | | | | 85±5 |  |
|  |  | |  | |  |  |  |  | |  |  | | | |  |  |
|  | Medium | | 300±10 | |  | 0.21±0.01 |  | 0.28±0.01 | |  | 0.37±0.01 | | | | 95±5 |  |
|  |  | |  | |  |  |  |  | |  |  | | | |  |  |
|  | Large | | 300±10 | |  | 0.21±0.01 |  | 0.28±0.01 | |  | 0.37±0.01 | | | | 105±5 |  |
|  | X Large | | 300±10 | |  | 0.21±0.01 |  | 0.28±0.01 | |  | 0.37±0.01 | | | | 115±5 |  |
|  | XX Large | | 300±10 | |  | 0.12±0.01 |  | 0.28±0.01 | |  | 0.37±0.01 | | | | 120±3 |  |
|  | XXX Large | | 300±10 | |  | 0.12±0.01 |  | 0.28±0.01 | |  | 0.37±0.01 | | | | 127±3 |  |

|  |  |  |
| --- | --- | --- |
| **Tensile(MPA)** | **Elongation(%)** | **Force At Break(N)** |
| **21 Mpa Min** | **700 %** | **≥ 6N** |

**Tensile (ASTM D412 & EN 455-2)**

**Before Aging**

**After Accelerated Aging**

|  |  |
| --- | --- |
| **Tensile(MPA)** | **Elongation(%)** |
| **18 Mpa min** | **500%** |

**Packaging**

|  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Total Residue Content** | | | | |  |  | <= 2.0 Milligrams per glove | | | |
| **Packaging (Normal)** | | | | |  |  | - 50 pieces in one Dispenser Box/Poly Bag | | | | |
|  |  |  |  |  |  |  | 10 Dispenser Box / Poly Bag in one Carton | | | | |
| **Labeling on Dispenser (Normal)** - Product Name, Size, Lot no. Quantity, | | | | | | | | | | |
|  |  |  |  |  |  |  | Manufacturer’s address |  |  |  |
| **Labeling on Carton (Normal)** | | | | | | | - Product Name, Size, Lot no. Quantity,country of origin | | | |

**Container Loadability** (No MOQ in manufacturer owned brand in standard Packaging)

20FCL=980 Cartons,40 FCL=1980 Cartons.