**ORANGE GRIPPER PRODUCT SPECIFICATIONS**

****

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Name of Product** | **:** 7 MilPowder Free Nitrile Gloves,Gripper. | | | | |
| **Name of Manufacturer** : :Innovative Gloves Co. Ltd. Hatyai, Thailand | | | | |
| **Base Material** | : Nitrile. |
| **Characteristics** | : Non Sterile, Ambidextrous Beaded Cuff | | | |
| **Available Sizes** | : Small,Medium, Large, X-Large , XX- Large | | |
| **Surface** | : Tire Tread Textured. | |
| **Surface Treatment** | : Polymer Coating | |
| **Colour** | : Orange. |

|  |  |
| --- | --- |
|  |  |
|  |  |
|  |  |

**Physical Specifications:**

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Size | Length  (mm | Thickness(±0.01) mm  SINGLE WALL | | | | | Width (mm) |
| Tip | | Palm | | Cuff |
| Smooth Surface | Textured Surface | Textured Surface | Smooth Surface | |
| Small | 240±5 | 0.19±0.01 | 0.29±0.02 | 0.20±0.02 | 0.12±0.01 | | 85±5 |
| Medium | 240±5 | 0.19±0.01 | 0.29±0.02 | 0.20±0.02 | 0.12±0.01 | | 95±5 |
| Large | 240±5 | 0.19±0.01 | 0.29±0.02 | 0.20±0.02 | 0.12±0.01 | | 105±5 |
| X Large | 240±5 | 0.19±0.01 | 0.29±0.02 | 0.20±0.02 | 0.12±0.01 | | 115±5 |
| XX Large | 240±5 | 0.19±0.01 | 0.29±0.02 | 0.20±0.02 | 0.12±0.01 | | 125±5 |

**Tensile (ASTM D412 & EN 455-2)**

**Before Aging**

|  |  |
| --- | --- |
| **Tensile(MPA)** | **Elongation(%)** |
| **22 Mpa min.** | **500 Min.** |

**After Accelerated Aging**

|  |  |
| --- | --- |
| **Tensile(MPA)** | **Elongation(%)** |
| **22 Mpa min.** | **400 min.** |

**Packaging**

|  |  |  |  |
| --- | --- | --- | --- |
| **Total Residue Content** | | - < 2.0 Milligrams per glove |  |
| **Packaging (Normal)** | | - 50 pieces in one Poly Bag or Dispenser Box | |
|  |  | 10 Poly Bag or Dispenser Box in one Carton | |

**Labeling on Dispenser (Normal)** - Product Name, Size, Lot no. Quantity, Manufacturer’s address, Warning about Nitrile Allergy in rare individuals.

**Labeling on Carton (Normal)** - Product Name, Size, Lot no. Quantity, Country of Origin

**Container Loadability** (No MOQ in manufacturer owned brand in standard Packaging)

20FCL=1135 Cartons,40 FCL=2740 Cartons.